## Slide 1
RBS/Channeling and SIMS analysis of
Si:Au samples
G. Malladi, Jay Mathews, J. Warrender and H. Efstathiadis

## Slide 2: Sample Structure
Sample ID | Implantation Dose (cm-2)
SiAu1C | 1×1014
SiAu2D | 5×1014
SiAu5B | 1×1015
cross-sectional view
n-Si (100) wafers implanted at 50 keV with Gold at doses mentioned in the table.
Laser-melted area,
crystalline
As-implanted area,
Probably not crystalline
Estimated amorphous layer thickness from TRIM is about 40 nm
plan view

## Slide 3: RBS Data: SiAu1C

## Slide 4
Overlay of RBS&Channeling: As-implanted & Laser-melted regions
The peak due to amorphization (red) has reduced after laser-melting (blue)

## Slide 5
Overlay of RBS&Channeling: As-implanted & Laser-melted regions – Zoom in
Gold peak before and after laser-melting

## Slide 6
# | Thickness | Composition at. fraction | 
 |  | Si | Au
1 | 100 A | 1.000 | 0
2 | 400 A | 1.000 | 0.0008
3 | 20000 A | 1.000 | 0
Depth profile from XRUMP simulation
The Au atoms moved more towards the surface and lesser towards the bulk of sample after laser-melting.
The Au edge (from XRUMP) is around channel # 939.2, but much of the peak has moved beyond this after laser-melting. This has been the case for all the three samples.
Overlay of RBS&Channeling: As-implanted & Laser-melted regions – Zoom in

## Slide 7
χmin = aligned/random
0 channel | As-implanted | Laser-melted
χAu | 0.9627 | 0.6014
χhost(Si) | 0.1856 | 0.0575
f | 0.9542 | 0.5771
Fraction of atoms in the channel f = (χAu –χhost)/ (1- χhost)
Calculation of Atoms in the Channel
Most of the Au atoms which are in the silicon are occupying the interstitial sites in all the three samples.
The fraction of Au atoms in the channel has been calculated for all the samples.

## Slide 8: RBS Data: SiAu2D

## Slide 9
Overlay of RBS&Channeling: As-implanted & Laser-melted regions

## Slide 10
Overlay of RBS&Channeling: As-implanted & Laser-melted regions – Zoom in
Gold peak before and after laser-melting

## Slide 11
# | Thickness | Composition at. fraction | 
 |  | Si | Au
1 | 100 A | 1.000 | 0
2 | 400 A | 1.000 | 0.0035
3 | 20000 A | 1.000 | 0
χmin = aligned/random
0 channel | As-implanted | Laser-melted
χAu | - (>1) | 0.8351
χhost(Si) | 0.1900 | 0.0557
f | - | 0.8254
Fraction of atoms in the channel f = (χAu –χhost)/ (1- χhost)
Calculation of Atoms in the Channel

## Slide 12: RBS Data: SiAu5B

## Slide 13
Overlay of RBS&Channeling: As-implanted & Laser-melted regions

## Slide 14
Overlay of RBS&Channeling: As-implanted & Laser-melted regions – Zoom in
Gold peak before and after laser-melting

## Slide 15
# | Thickness | Composition at. fraction | 
 |  | Si | Au
1 | 100 A | 1.000 | 0
2 | 400 A | 1.000 | 0.0058
3 | 20000 A | 1.000 | 0
χmin = aligned/random
0 channel | As-implanted | Laser-melted
χAu | 0.9958 | 0.7058
χhost(Si) | 0.2129 | 0.0713
f | 0.9947 | 0.6842
Fraction of atoms in the channel f = (χAu –χhost)/ (1- χhost)
Calculation of Atoms in the Channel